| Scope: | Specification for Re-melt Unalloyed Aluminium Sows/Ingots & Aluminium Alloy Hardeners. |  |  |
| --- | --- | --- | --- |
| Keywords: | Area: Purchasing Foundry (General) External Supplier/Subcontractor | Process: Goods Receiving Charge/Melt | Quality Description: Purchasing Inspection & Testing (Receiving) |

THIS DOCUMENT IS LEVEL 4 OF THE COMPANY’S APPROVED QUALITY SYSTEM. ITS CONTENTS ARE MANDATORY. REQUESTS FOR CHANGE SHALL BE MADE ON A CHANGE CONTROL FORM OBTAINABLE FROM YOUR SUPERVISOR. THE TABLES, LISTS, INDEXES OR FORMS ARE ATTACHED TO THE LEADING PAGES.

- Authorisation.

### Process Owners:

### Foundry Technical Manager

Foundry Team Manager

### Quality Manager

- Purpose

2.1	Provide a specification for purchasing and verification of all incoming aluminium for remelt purposes.

2.1	To ensure material can be produced within the specification limits required by Alcoa Europe Rolled Products Group.

- Who is Responsible?

3.1	It is the responsibility of the Remelt Resource Manager, to order material to this database.

3.2	It is the responsibility of incoming inspection to ensure deliveries conform to this database.

3.3	It is the responsibility of all suppliers to supply material that conforms to this specification.

- Other relevant documents.

4.1 Level 2

QM-PU-01	-	Purchase of Goods & Services.

QM-RM-01	-	Remelting Process Scrap.

4.2 Level 4

DB-TQ-050	-	List of approved suppliers of critical items.

WI-TQ-009	- 	Supplier Approval and Monitoring.

FOR INTERNAL USE ONLY

- Amendments

Date                           Issue	Reason

20.02.68 		3

17.12.75                         4	Specification revised & updated

01.09.76                         5	CR5 included

07.02.77                         6	CR7 Mg & Zn included

08.09.77                         7	50/50 SP Cu for use in 7475 included.

16.04.81                         8	FRS included & Cr maxfor NC20 added.

28.06.82                         9	Spec.for Pure Aluminium included.

20.02.86                       10	Lithium max. of 0.0002% added.C120 inc.

31.03.89                       11	Issued in new S.M.P. form.

13.10.89                       12	Include 9% min for Mn in MN10.

09.10.91                       13	Update to include colour code change.

This new format/numbered practice replaces C110 which should be destroyed.

17.11.92                       14	Incorrect specification Page 8 - 99.85% Cu A1 Grade.

14.01.93                       15	Change in specification requirements as per meeting with LSM on 08.01.93.

09.06.93                       16	Change in ingot supplier identification system.

06.12.93                       17	Inclusion of rod grain refiner into hardener spec. WI and correction of error in mag. concentration of beryllium hardener.

21.06.94                       18	Al 99.5 is included as a result of audit PC 9402.

24.06.96                       19	To prevent excessive pick-up of Li from ingot.

19.07.96                       20	Add composition of 5Ti 1B hardener.

17.07.97                       21	To add MAG50. To add sodium levels to 99.50, 99.70 and 99.92% Al grades. To add Lithium level to 99.50 Al grade after Russian Aluminium bought by group with unconfirmed analysis. To remove SR20 and replace with SR30. To remove CR4.

18.05.98                       22	To relax  limits on Iron & Silicon to allow lower purity based metal in hardener production.

16.09.98                       23	Rationalisation of hardener specs within BAL Group. 6%Zr, 12%Si and MN10A added to ACL. Main element ranges

tightened throughout.

20.11.98                       24 	Additional hardeners MAG 95 - 95% Mg Hardener, CAAL 10% Calcium Waffle, TICAL 315 ROD.

11.10.99                       25	Change 3.1 from Purchasing Manager to Remelt Resource Manager. CAR Audit QA9812. Add Zirconium grain refiner. Add Lithium. Addition of ALTAB Hardeners.

20.02.01                       26	New hardener Mg-Al-Mn. Change to Zr specification in accordance with process capability. To define maximum limits for trace elements.

22.08.01                       27	Bring 99.92% Alum Spec in line with AA192A Spec, apart from Na which is 0.002% max.

15.10.02                       28	Update to new format.  Fe was reduced from 0.20% max to 0.15% max at request of BASE.  This lower level restricts supply and is not necessary for Kitts Green products.

14.04.03                       29	Al grade 99.96% min added.  Selenium max of 0.0500added to MN10, MN10A and MN80 hardeners.

28-06.04		30		Re-ordered alpha numerically.  Grain refiner spec. 						composition amended, grain size and specific supplier 						specifications included.  Relaxed Zr limits on Zr5.  New 						Titanium hardener.  85% Manganese hardener added.

16.08.07		31		Note re cleanliness added.  Paragraph re  Beryllium Hardener 					removed on page 6.

18.02.09		32		Remove MRA 40% Copper, MAG 50, MAG 95, Mg-Al-Mn, 					MN10A, MN80, ALTAB, 12% Silicon, ZR6, SR20%, TICAL, 					V5.  Amend Tygem to read Titanium Tablet, 5Ti 0.2B grain 					refinement rod to have grain size of 160 microns. Salts based 					process specified for ZR5

07.05.10		33		Change to Prime compositions to comply with commercial 					grades. Introduction of a specification for Copper.  						Information for suppliers as per AS9100 requirements

29.02.12		34		Modification to grain refiner rod targets in line with Alcoa 						specs – MS 1-2251 STi  1b, MS 1-2207 STi 0.2B, MS 1-224 					3Ti 13

15.03.12		35		CR80 F89 & Mn85 Min. Target & max added.

24.07.12		36		Change min% vanadium to 9.0% to align with Alcoa alloying 					materials specifications.

24.10.12		37		Note 11 for Suppliers and Receiving Inspection.  Addition of 					“regulatory authorities” to comply with AS9100

09.12.13		38		Change to CAAL 10% Calcium Waffle.

27.06.14		39		Add Ty-gem specification (88% min Ti).

31.10.14		40		Added P0303 specification. Notes on chemical analysis (rare 					earth elements) and WI-TQ-009 to relevant documents list.

26.02.15		41		Increase Na limit of all prime grades from 20 to 40 ppm max.

24.03.15		42		Added 99.67 (P1320) grade alum as a specific concession.

6     Distribution List

Internal

72, 67, 29, 14, 43, 62, 56, 101

External

R Dodd – Swansea

All approved critical suppliers categories 0A, 1B, 1Bi, 1E

Notes for Suppliers and Receiving Inspection

1.	The chemical composition shall comply with the limits appended.

2.	An analytical release certificate shall be provided for each furnace melt and each melt shall be clearly identified.

3.	Analytical checks shall be carried out at the discretion of the Foundry Technical Manager.

4.	A bundle of ingots shall only contain the product of 1 melt.

5.	Each ingot in a bundle shall be identified with its own colour code except where stated in this practice.

6.	The ingots are to be held in a properly organised store area and every precaution taken to prevent mixing and contamination.

7.	Remelt sows and ingots shall be stacked with base uppermost to reduce the risk of water seeping into sumps.

8.	All unalloyed aluminium sows/ingots and alloy hardeners shall be clean and free of corrosion.

9.	The supplier shall notify Alcoa Flat Rolled Products – Kitts Green of any non-conforming 	product and must only ship such product if formal approval is granted.

10.	The supplier shall notify Alcoa Flat Rolled Products – Kitts Green of any changes in the 	product or process which may affect the quality or performance of the product being supplied.

11.	Periodic surveys of the supplier’s Quality Management System, product(s) and/or process(es) 	may be undertaken by authorised representatives of Alcoa Flat Rolled products, its 		customers and/or regulatory authorities, who will require access to the applicable areas of all 	the supplier’s premises at all reasonable times.

12.	It is expected that suppliers will retain records relating to the manufacturing of the product in 	the event of any quality issue arising from use of the product.  Records shall be maintained 	for a minimum of 5 years.

Aluminium Ingot

Grade 99.50				Grade 99.70

| AL Grade (Max.Limits Wt%)(1) | P1535A |  | AL Grade (Max.Limits Wt%)(1) | P1020A |
| --- | --- | --- | --- | --- |
| Iron | 0.35 |  | Iron | 0.20 |
| Silicon | 0.15 |  | Silicon | 0.10 |
| Zinc | 0.03 |  | Zinc | 0.03 |
| Vanadium | 0.02*^ |  | Vanadium | 0.02*^ |
| Gallium | 0.04 |  | Gallium | 0.04 |
| Sodium | 0.004* |  | Sodium | 0.004* |
| Lithium | 0.0002* |  | Lithium | 0.0002* |
| Cd + Pb + Hg | <0.010 |  | Cd + Pb + Hg | <0.010 |
| Aluminium | Rest |  | Aluminium | Rest |
| Others Each | 0.03 |  | Others Each | 0.03 |
| Others Total | 0.10 |  | Others Total | 0.10 |

Grade 99.84				Grade 99.90

| AL Grade (Max.Limits Wt%) (1) | P0610A |  | AL Grade (Max.Limits Wt%)(1) | P0406A |
| --- | --- | --- | --- | --- |
| Iron | 0.10 |  | Iron | 0.06 |
| Silicon | 0.06 |  | Silicon | 0.04 |
| Zinc | 0.03 |  | Zinc | 0.03 |
| Vanadium | 0.02 |  | Vanadium | 0.02 |
| Gallium | 0.04 |  | Gallium | 0.03 |
| Sodium | 0.004* |  | Sodium | 0.004* |
| Lithium | 0.0002* |  | Lithium | 0.0002* |
| Cd + Pb + Hg | <0.010 |  | Cd + Pb + Hg | <0.010 |
| Aluminium | Rest |  | Aluminium | Rest |
| Others Each | 0.02 |  | Others Each | 0.02 |
| Others Total | 0.05 |  | Others Total | 0.04 |

Grade 99.92				Grade 99.94			Grade 99.96

| AL Grade (Max.Limits Wt%) (1) | P0404A |  | AL Grade (Max.Limits Wt%) (1) | P0303A |  | AL Grade (Max.Limits Wt%) (1) | P0202A |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Iron | 0.04 |  | Iron | 0.03 |  | Iron | 0.02 |
| Silicon | 0.04 |  | Silicon | 0.03 |  | Silicon | 0.02 |
| Zinc | 0.03 |  | Zinc | 0.02 |  | Zinc | 0.02 |
| Vanadium | 0.01 |  | Vanadium | 0.01 |  | Vanadium | 0.01 |
| Gallium | 0.03 |  | Gallium | 0.02 |  | Gallium | 0.02 |
| Sodium | 0.004* |  | Sodium | 0.004* |  | Sodium | 0.004* |
| Lithium | 0.0002* |  | Lithium | 0.0002* |  | Lithium | 0.0002* |
| Cd + Pb + Hg | <0.010 |  | Cd + Pb + Hg | <0.010 |  | Cd + Pb + Hg | <0.010 |
| Aluminium | Rest |  | Aluminium | Rest |  | Aluminium | Rest |
| Others Each | 0.01 |  | Others Each | 0.01 |  | Others Each | 0.01 |
| Others Total | 0.03 |  | Others Total | 0.02 |  | Others Total | 0.02 |

Note1       Metal falling outside the limits must be made the subject of a concession.

(* Kitts Green Specific Requirement)

(^Levels up to 0.03 are acceptable, but restrictions will apply on the amounts used in the charge make up)

NB Aluminium Grades 99.50 (P1535A), 99.70 (P1020A), 99.84 (P0610A), 99.90 (P0406A), 99.92 (P0404A), 99.94 (P0303A) and 99.96 (P0202A) represent the standard grades purchased by Kitts Green.  When a particular grade is unavailable it may be substituted by a grade of higher purity. The substitution must meet or exceed the requirements of the standard grade it replaces.

99.67 (P1320 grade) is not normally purchased by Kitts Green, but can be accepted on concession. The individual lot chemistries shall be checked before material arrives on site, and if the actual analysis of any specific batch is found to not meet the requirements of 99.70 grade, (see above), then this batch shall be segregated, identified specifically on Keystone, and consumed only in suitable alloys.

Grade 99.67

| AL Grade (Max.Limits Wt%) | P1320A |
| --- | --- |
| Iron | 0.20 |
| Silicon | 0.13 |
| Zinc | 0.03 |
| Copper | 0.04 |
| Vanadium | 0.05 |
| Gallium | 0.04 |
| Sodium | 0.004* |
| Lithium | 0.0002* |
| Cd + Pb + Hg | <0.010 |
| Aluminium | Rest |
| Others Each | 0.03 |
| Others Total | 0.10 |

Chemical Analysis

Raw materials used in Kitts Green remelt operations are tested annually to ensure the quality of supply (see WI-TQ-009). Materials shall be tested against the relevant purchasing specifications, (detailed in this document), to ensure that the materials are as described and that the supplied analysis is consistent. In addition, materials will also be checked for the following heavy, toxic and rare earth elements;

Arsenic (Ac), Molybdenum (Mo), Cadmium (Cd), Mercury (Hg), Beryllium (Be), Lithium (Li), Lead (Pb), Cerium (Ce), Neodymium (Nd), Uranium (U), Praseodymium (Pr) and Lanthanum (La).

Aluminium Alloy Hardeners

CAAL 10% Calcium Waffle (Colour code - Nil)

Min % 		Max %

Calcium 		9.0	          	11.00

Iron	 -		0.20

Silicon	 - 		0.10

Lithium	 - 		0.0002

Magnesium				 -		0.20

Others

Each	 -		0.05

Total	 -		0.15

Aluminium the remainder

CR5 - 5% Chromium Hardener (Colour code - Green/Yellow)

Min % 		Max %

Chromium 	5.0 		5.5

Copper  	- 		0.05

Iron  	-  		0.15

Magnesium 	-  		0.05

Manganese 	- 		0.05

Silicon	- 		0.10

Zinc  	- 		0.05

Titanium 	- 		0.05

Nickel 	- 		0.05

Lead	- 		0.05

Bismuth 	-		0.05

Lithium	- 		0.0002

Others

Each	-		0.03

Total	-		0.15

Aluminium the remainder

CR20 - 20% Chromium Hardener (Colour code - Purple)

Min%		Max%

Copper					-		0.10

Iron					-		0.55

Magnesium				-		0.05

Manganese				-		0.05

Silicon	-		0.30

Zinc					-		0.05

Titanium				-		0.05

Chromium				20.0		22.0

Lithium					-		0.0002

Others

Each	-		0.05

Total	-		0.15

Aluminium the remainder

CR80 ALTAB Hardener (Colour code - Blue)

Min%		Target%	Max%

Cr       			79		    80		  81

Aluminium the remainder

Copper Pure (Cu-CATH-1 or equal)

Min %                 Max %

Copper 	99.9		-

Bale Weight not to exceed 25kg

50/50 Super Purity Copper Hardener (Colour code - Red/White)

Min %                 Max %

Copper 	50.0		52.0

Iron	-		0.08

Magnesium	- 		0.10

Manganese	-		0.10

Silicon	-		0.07

Nickel	-		0.05

Titanium	-		0.05

Zinc	-		0.05

Lead	-		0.05

Bismuth	-		0.05

Lithium		-	           0.0002

Others

Each	-		0.03

Total	-		0.15

Aluminium the remainder

FR4 - 4% Iron Hardener (Colour code - Black/White)

Min % 		Max %

Iron 	4.0		4.5

Copper 	- 		0.20

Magnesium 	-		0.20

Manganese 	-		0.20

Silicon 	-		0.30

Nickel	-		0.10

Titanium 	- 		0.10

Zinc	- 		0.10

Lead 	- 		0.10

Bismuth	- 		0.10

Lithium			0.0002

Others

Each	-		0.03

Total	-		0.15

Aluminium the remainder

FR80 ALTAB Hardener   (Colour code - Green)

Min%		Target%	Max%

Fe       					 79		    80		  81

Aluminium the remainder

Lithium Metal

Chemistry

Min % 		Max %

Sodium		-		<120 ppm

Potassuim		-		<100 ppm

Calcuim                                       	-		<120 ppm

Iron		-		<10 ppm

Chlorine		-		<50 ppm

Nitrogen		-		<300 ppm

Others each		-		<100 ppm

Others max		-		<1300 ppm

Lithium	(balance by difference)

Size:

Weight               	1kg

Dimensions        	100mm dia.       250mm length

Packaging

Dry packed in Argon sealed individually in 1kg units.

NB

- Alternative size/weight ingots to be agreed by production.

- No wax/paraffin packaging acceptable.

Pure Magnesium  (99.8% min) (Colour code - Nil)

Min%		Max %

Copper 			-		0.02

Lead			-		0.01

Manganese 			-		0.10

Nickel 			-		0.001

Tin 			-		0.01

Others			-		0.05

Magnesium the remainder. Purchased to specification ASTM B92.998OA.

Ingots to be free of corrosion.

MN10 - 10% Manganese Hardener (Colour code - Brown/Black)

Min %             Max %

Manganese 	10.0		11.0

Copper 	-		0.10

Iron	-		0.40

Magnesium 	-		0.25

Silicon	-		0.40

Nickel	-		0.10

Zinc 	- 		0.20

Lead	- 		0.10

Bismuth 	-		0.10

Titanium 	- 		0.20

Lithium	- 		0.0002

Selenium				-		0.0500

Others

Each	-		0.03

Total	-		0.15

Aluminium the remainder

MN85 ALTAB Hardener (Colour code – Silver)

Min%		Target%	Max%

Mn					  84	     	    85		   86

Selenium					   -				0.0500

Aluminium the remainder

NC20 - 20% Nickel Hardener (Colour code - Blue/Red)

Min % 		Max %

Nickel                                                       20.0 		22.0

Copper					-		0.50

Iron                                                           -		0.50

Magnesium				-		0.25

Manganese				-		0.25

Silicon					-		0.25

Zinc					-		0.10

Lead					-		0.10

Bismuth				-		0.10

Titanium				-		0.10

Chromium				-		0.10

Lithium					-		0.0002

Others

Each			0.03

Total			0.15

Aluminium the remainder

SR30 - 30% Silicon Hardener (Colour code - Yellow/Blue)

Min %               Max %

Silicon                       			30.0                	32.0

Copper 	-		0.20

Iron	-		0.40

Magnesium	-		0.20

Manganese	-		0.20

Nickel	-		0.10

Zinc 	-		0.10

Lead	-		0.10

Bismuth	-		0.10

Titanium	-		0.10

Lithium 	-		0.0002

Others

Each	-		0.03

Total	-		0.15

Aluminium the remainder

TR6 -6% Titanium Hardener (Colour Code - Blue/Green)

Min % 		Max %

Titanium		6.0		6.5

Iron	-		0.3

Silicon	-		0.1

Vanadium	-		0.3

Bismuth	-		0.004

Lithium 	-		0.0002

Others

Each	-		0.05

Total	-		0.15

Aluminium the remainder

Titanium Tablet (Colour code – none)

Min%		Max%

Titanium				92.0		98.0

Ty-Gem Titanium Tablet (Colour code – Red)

Min%		Max%

Titanium				>88.0

Silicon					-		0.3

Iron					-		1.0

Chromium				-		0.3

Nickel					-		0.3

Molybdenum				-		0.3

Tin					-		0.3

Vanadium				-		3.0

Zirconium				-		0.3

Lead + Cadmium + Mercury		-	           <0.010

Beryllium				-		0.0001

Lithium					-		0.0002

Moisture				-		0.05

Others

Each					-		0.03

Total					-		0.10

5Ti 1.0B grain refining rod (Colour code - green)

Min %		Target%		Max %

Titanium	4.8		5.0			5.2

Boron	0.8		1.2			1.2

Iron	-					0.30

Silicon	-					0.20

Vanadium	-					0.01

Lead + Cadmium			-					<0.01

Beryllium				-					0.0001

Others

Each	-					0.03

Total	-					0.10

Aluminium the remainder

Ability to achieve grain size of 140 micron or less in one min. using the standard AA TP 1 test.

Specific detailed supply specification to be agreed with each approved supplier.

5Ti 0.2B grain refining rod (Colour code - green/black)

Min %		Target%		Max %

Titanium	4.8		5.0			5.2

Boron	0.17		0.20			0.23

Iron	-					0.30

Silicon	-					0.20

Vanadium	-					0.15

Lead + Cadmium			-					<0.01

Beryllium				-					0.0001

Others

Each	-					0.03

Total	-					0.10

Aluminium the remainder

Ability to achieve grain size of 160 micron or less in one min. using the standard AA TP 1 test.

Specific detailed supply specification to be agreed with each approved supplier.

3Ti 1.0B grain refining rod (Colour code - green/brown)

Min %		Target %		Max %

Titanium	2.8		3.1			3.4

Boron	0.7		0.9			1.1

Iron	-		-			0.30

Silicon	-		-			0.20

Vanadium	-		-			0.15

Lead + Cadmium			-		-			<0.010

Beryllium				-		-			0.0001

Others

Each	-		-			0.03

Total	-		-			0.10

Aluminium the remainder

Ability to achieve grain size of 140 micron or less in one min. using the standard AA TP 1 test.

Specific detailed supply specification to be agreed with each approved supplier.

V10-10% Vanadium Hardener (Colour code - Purple/White)

Min % 		Max %

Vanadium	9.0		11.0

Copper 	- 		0.20

Iron        	- 		0.40

Magnesium 	- 		0.25

Manganese 	- 		0.25

Silicon 	- 		0.40

Zinc	-		0.20

Titanium	- 		0.20

Nickel 	- 		0.10

Lead	-		0.10

Bismuth 	- 		0.10

Lithium 	- 		0.0002

Others

Each	-		0.03

Total	-		0.15

Aluminium the remainder

Pure Zinc (99.95% min.) (Colour code - Nil)

Min % 		Max %

Cadmium   				-		0.02     )

Iron 			-		0.01     )

Lead					0.03     ) Max total of 0.05%

Tin  			-		0.001   )

Zinc the remainder. Purchased to specification BS3436 Zn 2(99.95%).

ZR5 - 5% Zirconium Hardener (Colour code - Yellow/Red)

Min % 		Max %

Zirconium -	4.8 		5.4

Copper 	-		0.20

Iron 	- 		0.20

Magnesium 	-		0.25

Manganese	-		0.25

Silicon	- 		0.40

Zinc	-		0.20

Titanium	-		0.20

Nickel	- 		0.10

Lead	-		0.10

Bismuth	-		0.10

Lithium	- 		0.0002

Others

Each	-		0.03

Total	-		0.15

Aluminium the remainder

Manufactured using a salts based process.

Zygem Zirconium Tablets (Colour code - Blue)

Min % 		Max %

Zirconium 		92.00 	        	100.00

Titanium	-		3.50

Vanadium 	- 		0.10

Silicon	- 		0.20

Chromium	-		0.10

Nickel	- 		0.30

Iron	-		0.50

Lead	-		0.01

Tin	-		0.15

Others

Each	-		0.03

Total	-		0.15

Aluminium the remainder